## Slide 1: Performance specifications for cementitious grouts used in post-tensioned concrete systems
  Manu K. MOHAN, M. S. Student
  Radhakrishna G. PILLAI, Associate Professor
  Manu SANTHANAM, Professor
  Ravindra GETTU, Professor
Indian Institute of Technology Madras
Chennai, INDIA
September 19-22, 2018
  ICI-IWC 2018
  NIMHANS convention center, Bangalore, India
Ministry of Human Resource Development and
Ministry of Housing and Urban Affairs
Government of India

## Slide 2: Grouted, post-tensioned (PT) systems are commonly used in large concrete structures
Source : https://www.google.co.in and FDOT report (2003)
High-rise buildings
Nuclear vaults
Long-span segmental bridges
Silos
Strands are embedded in plastic ducts and the interstitial spaces are supposed to be filled with grout

## Slide 3: Premature corrosion has been observed in many YOUNG bridges
Mandovi, 12
Ynys-y-Gwas, 33
Malle, 13
Bickton Meadows, 15
Niles Channel, 16
Mid Bay,15
447 bridges in UK
Ban during 1992 – 1996
(Woodward, 1988)

## Slide 4: Premature corrosion has been observed in many YOUNG bridges
Varina-Enon, Virginia
At 17 years
FDOT 2003
Anchorage zone in a PT girder

## Slide 5: Premature corrosion has been observed in many YOUNG bridges
Sunshine Skyway, Florida
At 8 years
FDOT 2001
Anchorage zone in PT column

## Slide 6: Why such premature corrosion? Voids in ducts  exposed strands
Anchorage zone in a PT girder
Anchorage zone in PT column
A metro rail bridge

## Slide 7: Why such premature corrosion? Chloride ingress  Corrosion of strands
Chlorides

## Slide 8: Why such premature corrosion? Carbonation of ‘top’ grout  Localized corrosion
CO2

## Slide 9: Are the new grouts good enough? - Formation of soft grout should be avoided
Inadequate specs.  Voids  Premature corrosion

## Slide 10: Methods to assess the fluidity and its retention of PT grouts
Flow cone test
Spread test
Flow cone (EN445:2007)
Grout spread
(EN445:2007)
Cylinder
Smooth plate

## Slide 11: Methods to assess the bleed resistance of PT grouts
Standard bleed (SB) test
Wick-induced bleed (WB) test
Pressure-induced bleed (PB) test
Inclined tube bleed (IT) test
Standard bleed (SB) test
Pressure-induced
Bleed (PB) test
Inclined-tube test
Wick-induced
bleed (WB) test
PCG = Plain cement grout
SBG = Site batched grout
PPG = Pre-packed grout (commercial)
TF = Tendon Fill

## Slide 12: Fluidity (Efflux time, T0) of commercial grouts
TF
PCG = Plain cement grout
SBG = Site batched grout
PPG = Pre-packed grout (commercial)
TF = Tendon Fill
Good quality PT grouts may get disqualified by the current efflux time test and viceversa !
We have to use other tests to qualify/disqualify PT grouts
Kamalakannan et al 2018

## Slide 13: Recommended specifications for fluidity and its retention
Flow cones with smaller orifice diameters
Thixotropic grouts with very low w/c
Property | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | Recommended
Efflux time, T0 (s) | T0 ≤ 25 (EN 445 Flow cone) | T0 ≤ 25 | 5 ≤ T0 ≤ 30 (ASTM C939 Marsh cone) | T0 ≤ 25 (EN 445 Flow cone)
Efflux time 30 min. after mixing, T30 (s) | 1.2 T0 ≥ T30 ≥ 0.8 T0 and T30 ≤ 25 | Not mentioned | Not mentioned | 1.2 T0 ≥ T30 ≥ 0.8 T0 and T30 ≤ 25
Efflux time 180 min. after mixing, T180 (s) | Not mentioned | Not mentioned | Not mentioned | 1.4 T0 ≥ T180 ≥ 0.6 T0 and T180 ≤ 25
2 mm orifice
Notes: Depending on the pre-shear (past shear histories applied on the grout), the fluidity will change as it’s a thixotropic material.
The green colour indicates the recommended specification.

## Slide 14: Mixture proportion of the grouts studied
Material | Quantity (kg/m3) |  |  |  |  |  |  |  | 
 | PPG1 | PPG2 | PPG3 | PPG4 | PPG5 | PPG6 | PPG7 | PPG8 | PPG9
OPC | 1473 | 1120 | 1088 | 1119 | 951 | 951 | 951 | 951 | 951
Fly ash-1 (Class F) | 0 | 320 | 512 | 0 | 317 | 317 | 317 | 317 | 317
Fly ash-2 (Class F) | 0 | 0 | 0 | 480 | 317 | 317 | 317 | 317 | 317
Silica fume | 164 | 160 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Water | 458 | 432 | 432 | 432 | 428 | 428 | 428 | 428 | 428
HRWR | 1.80 | 1.44 | 1.44 | 1.43 | 1.43 | 1.53 | 1.43 | 1.43 | 1.43
Viscosity modifier | 0 | 0 | 0.80 | 0.79 | 0.50 | 0 | 0.80 | 0.63 | 0.63
Nano clay | 0 | 0 | 0 | 0 | 0 | 1.58 | 0 | 0 | 0
SRA | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 31.7
water/binder | 0.28 | 0.27 | 0.27 | 0.27 | 0.27 | 0.27 | 0.27 | 0.27 | 0.27

## Slide 15: Fluidity and its retention
PPGs 1, 2, and 3 met the requirements
Grouts with low efflux time need not have required fluidity retention (e.g., PPG6)
Grout | T0 | T30 | T180
PPG 1 | 12 | 13 | 19
PPG 2 | 14 | 15 | 24
PPG 3 | 18 | 19 | 25
PPG 4 | 29 | 30 | 37
PPG 5 | 24 | 26 | 27
PPG 6 | 15 | 18 | 28
1.2 T0 ≥ T30 ≥ 0.8 T0 and T30 ≤ 25
1.4 T0 ≥ T180 ≥ 0.6 T0 and T180 ≤ 25
×
×
×
Acceptance criteria
PPG = Pre-packaged grout

## Slide 16: Recommended specifications for fluidity (Spread, S)
Rarely used, though a simple test
Property | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | Recommended
Grout spread, S0 (mm) | S0 ≥ 140 | S0 ≤ 25 | 5 ≤ S0 ≤ 30 (ASTM C939 Marsh cone) | S0 ≤ 25 (EN 445 Flow cone)
Grout spread 30 min. after mixing, S30 (mm) | 1.2 S0 ≥ S30 ≥ 0.8 S0 and S30 ≥ 140 | Not mentioned | Not mentioned | 1.2 S0 ≥ S30 ≥ 0.8 S0 and S30 ≤ 25
Grout spread 180 min. after mixing, S180 (mm) | Not mentioned | Not mentioned | Not mentioned | 1.4 S0 ≥ S180 ≥ 0.6 S0 and S180 ≥ 120

## Slide 17: Fluidity and its retention (Spread, S)
Grout | S0 | S30 | S180
PBG 1 | 167 | 161 | 141
PBG 2 | 158 | 153 | 136
PBG 3 | 151 | 146 | 122
PBG 4 | 117 | 114 | 86
PBG 5 | 128 | 121 | 90
PBG 6 | 160 | 151 | 130
PPGs 1, 2, 3, and 6 met the requirements
×
×
1.2 S0 ≥ S30 ≥ 0.8 S0 and S30 ≥ 140
1.6 S0 ≥ S180 ≥ 0.6 S0 and S180 ≥ 120
Acceptance criteria

## Slide 18: Recommended specifications for bleed resistance
Property | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | Recommended
Bleed (%) |  |  |  | 
Standard | Not mentioned | Not mentioned | ≤ 0.1 | ≤ 0.1
Wick-induced | ≤ 0.3 | ≤ 0.3 | ≤ 0.3 | ≤ 0.0
Wick-induced bleed test
Standard bleed test
Standard bleed and wick-induced bleed tests must be done

## Slide 19: Recommended specifications for bleed resistance
Property | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | Recommended
Bleed (%) |  |  |  | 
Pressure-induced (at 350 kPa) | Not mentioned | Not mentioned | ≤ 0.1 | ≤ 0.1
Inclined tube test | ≤ 0.3 | ≤ 0.3 | ≤ 0.3 | ≤ 0.3

## Slide 20: Bleed resistance of existing PPGs and other indigenous grouts
PT grouts used in today’s construction industry do not meet the recommended specifications
Upper limit = 0.3 %
(EN 447:2007)
Kamalakannan et al. 2018, Ashok 2015, Ramya, 2015

## Slide 21: Bleed resistance of the grouts
PPG3 and PPG5 has very low bleed and can be used for PT columns
×
×

## Slide 22: Recommended specifications for dimensional stability
Compressive strength is not a screening test
Good dimensional stability
  Total and autogenous shrinkage
Property | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | Recommended
Compressive strength (MPa) |  |  |  | 
7-day | ≥ 27 | ≥ 27 | ≥ 21 | ≥ 21
28-day | ≥ 30 | Not mentioned | ≥ 35 | ≥ 35
Hardened volume change (%) |  |  |  | 
Expansion | Not mentioned | Not mentioned | ≤ 0.1 at 24 hours ≤ 0.2 after 28 days | ≤ 0.1 at 24 hours ≤ 0.2 after 28 days
Shrinkage | Not mentioned | Not mentioned | Not mentioned | ≤ 0.2 after 28 days
ASTM C1090 test for measuring expansion
ASTM C157 specimens for measuring the shrinkage

## Slide 23: Cube compressive strength and shrinkage for the grouts
PPG4 has highest compressive strength; PPG6 has lowest
Shrinkage strains were reduced with the use of SRA
Total shrinkage
Autogenous shrinkage

## Slide 24: Visual observations on grout cylinders/tendons can also be used as performance tests
Frothy material floats or forms at the top surface of grout
Ashok Gorantla 2016, http://www.fhwa.dot.gov/publications/research/infrastructure/structures/bridge/13028/
Segregation in
the lab specimens
Segregation in the field tendons

## Slide 25: Modified performance specifications for PT grouts
Parameter |  | Acceptance criteria | Test method | Standard
Fresh state (very crucial) | Efflux time, T0 (s) | T0 ≤ 25 | Flow Cone test as per EN 445:2007 | EN 447:2007
 | Efflux time 30 minutes after mixing, T30 (s) | 1.2 T0 ≥ T30 ≥ 0.8 T0 and T30 ≤ 25 |  | 
 | Efflux time 180 minutes after mixing, T180 (s) | 1.4 T0 ≥ T180 ≥ 0.6 T0 and T180 ≤ 28 |  | 
 | Gout spread, S0 (mm) | ≥ 140 | Grout spread test as per EN 445:2007 | 
 | Grout spread 30 minutes after mixing, S30 (mm) | 1.2 S0 ≥ S30 ≥ 0.8 S0 and S30 ≥ 140 |  | 
 | Grout spread 180 minutes after mixing, S180 (mm) | 1.4 S0 ≥ S180 ≥ 0.6 S0 and S180 ≥ 120 |  | 
 | Bleed (%) |  | Standard, wick bleed and inclined tube test as per EN 445:2007 Pressure-induced bleed test as per ASTM C1741 | EN 447:2007 and PTI M55.1-12
 | Standard | - |  | 
 | Wick-induced | ≤ 0.3 |  | 
 | Pressure-induced (at 350 kPa) | ≤ 0.1 |  | 
 | Inclined tube | ≤ 0.3 |  | 
 | Setting time (hrs.) |  | Setting time test as per ASTM C953 | EN 447:2007 and PTI M55.1-12
 | Initial | ≥ 3 |  | 
 | Final | ≤ 24 |  | 

## Slide 26: Modified performance specifications for PT grouts
Parameter |  | Acceptance criteria | Test method | Standard
Desired | Compressive strength (N/mm2) |  | ASTM C942 with the moulds complying to ASTM C 109 | EN 447:2007 and PTI M55.1-12
 | 3 day | ≤ 10 |  | 
 | 7 day | ≤ 27 |  | 
 | 28 day | ≤ 30 |  | 
Very Crucial | Hardened volume change (%) |  | ASTM C1090 for expansion and ASTM C157 or ASTM C1698 for shrinkage | PTI M55.1-12
 | Expansion | ≤ 0.1 at 24 hours & ≤ 0.2 after 28 days |  | 
 | Shrinkage | ≤ 0.2 after 28 days |  | 
Crucial | Deleterious ions (% of binder) |  | Ion Chromatography or Chemical analysis | EN 447:2007 and PTI M55.1-12
 | Chloride (Cl2-) | ≤ 0.08 |  | 
 | Sulphates (SO42-) | ≤ 4.00 |  | 
 | Sulphides (S2-) | ≤ 0.01 |  | 
A set of stringent specifications must be used to achieve good quality PT grout

## Slide 27: Avoid the filling of duct with water before grouting
Chances are very less that the grout will entirely displace the water
Strands may get corroded and left as it is
  There may be significant delays between the placing of strands in the duct and the prestressing
Ashok Gorantla 2016
Signs of strand corrosion in a duct that was filled with water
water filled duct prior to grouting
Vent
water flow
water flow
Increasing gradient
Inlet


## Slide 28: Grout must be pumped from the lowest points to get complete filling of the duct
Vent
Dead end anchorage
Duct
Stressing anchorage
Inlet
Vents
Inlet
Vent
Min.
1 m
Grout flow
Grout flow
Grout flow
Grout flow
Increasing gradient

## Slide 29: Grout flowing out of the other end does not mean that the tendon is filled with grout
A simplified schematic of typical tendon profile (Not to scale)

## Slide 30: Void formation can be avoided by keeping anchors “face-down” and appropriate vents



## Slide 31: Cementitious cover/cap can attract humidity and moisture and cause corrosion near the ends
http://www.fhwa.dot.gov/bridge/pt/pt.pdf
PT systems with ends covered with cementitious materials

~ 13 years!
Crack-resistant bituminous coating is better than cementitious coating

Severe corrosion at the anchorages

## Slide 32: Conclusions
Efflux time alone should not be used to disqualify a thixotropic grout
Bleed resistance is very important to avoid void formation inside the ducts
Retention of flow/bleed resistance are important to check
A set of stringent performance specifications can significantly improve the quality of the PT grouting and life of PT bridges.
PT grouts developed in this study meets all the critical specifications and the grouts have a good balance between the fluidity and the bleed resistance.
The grouting practices are also very important
Future work
  Specifications with smaller orifices and their correlation with bleed

## Slide 33: Tendons are the backbone of pre- and post-tensioned concrete structures
We must do whatever we can to prevent corrosion of these expensive and important systems
– an extra care at the beginning in achieving this is really worth in the long term.
Thank You
pillai@iitm.ac.in

## Slide 34: Visit our stall
Thank You
(pillai@iitm.ac.in)

## Slide 35
Thank you

## Slide 36: Performance specifications for flowable cementitious grouts for post-tensioned concrete systems
  Manu K. Mohan, M. S. Student
  Radhakrishna G. Pillai, Associate Professor
  Manu Santhanam, Professor
  Ravindra Gettu, Professor
Indian Institute of Technology Madras
Chennai, INDIA
September 21, 2018
  Innovative world of Concrete (ICI-IWC 2018)
  NIHAMS convention center, Bangalore, India

## Slide 37: Specifications for PT grouts from various standards were reviewed
Property |  | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | MORTH (2005) | IRS (1997) | IS 1343 (2012)
Fresh | Efflux time, T0 (s) | T0 ≤ 25 (EN 445 Flow cone) | T0 ≤ 25 | 5 ≤ T0 ≤ 30 (ASTM C939 Marsh cone) | - | - | -
 | Efflux time 30 minutes after mixing, T30 (s) | 1.2 T0 ≥ T30 ≥ 0.8 T0 and T30 ≤ 25 | - | - | - | - | -
 | Grout spread, S0 (mm) | S0 ≥ 140 | - | - | - | - | -
 | Grout spread 30 minutes after mixing, S30 (mm) | 1.2 S0 ≥ S30 ≥ 0.8 S0 and S30 ≥ 140 | - | - | - | - | -
 | Bleed (%) |  |  |  |  |  | 
 | Standard | - | - | ≤ 0.0 | - | - | -
 | Wick-induced | ≤ 0.3 | ≤ 0.3 | ≤ 0.0 | ≤ 0.3 | - | -
 | Pressure-induced (at 350 kPa) | - | - | ≤ 0.0 | - | - | -
 | Inclined tube test | ≤ 0.3 | ≤ 0.3 | ≤ 0.3 | - | - | -
 | Setting time (hours) |  |  |  |  |  | 
 | Initial (Ti) | Ti ≥ 3 | Ti > 3 | 3 ≤ Ti ≤ 12 | 3 ≤ Ti ≤ 12 | - | -
 | Final (Tf) | Tf ≤ 24 | Tf < 24 | - | Tf ≤ 24 | - | -

## Slide 38: Specifications for PT grouts from various standards were reviewed
Property |  | EN 447 (2007) & ISO 14824 (2012) | fib Bulletin No. 20 (2002) | PTI M55 (2003) | MORTH (2005) | IRS (1997) | IS 1343 (2012)
Hardened | Compressive strength (MPa) |  |  |  |  |  | 
 | 7-day | ≥ 27 | ≥ 27 | ≥ 21 | ≥ 28 | ≥ 17 | -
 | 28-day | ≥ 30 | - | ≥ 35 | ≥ 30 | - | ≥ 27
Dimensional stability | Hardened volume change |  |  |  |  |  | 
 | Expansion | - | - | ≤ 0.1 at 24 hours ≤ 0.2 after 28 days | - | - | -
 | Shrinkage | - | - | - | - | - | -
Durability | Deleterious materials (%) |  |  |  |  |  | 
 | Chloride (Cl-) | ≤ 0.10 | ≤ 4.10 | ≤ 0.08 | ≤ 0.1 | - | ≤ 0.1
 | Sulphate (SO32-) | ≤ 4.50 | ≤ 4.50 | - | ≤ 4 | - | -
 | Sulphide (S2-) | ≤ 0.01 | ≤ 0.01 | - | ≤ 0.01 | - | -
Most of the existing specifications are inadequate/not complete for developing a good quality PT grout

## Slide 39: Limitations of the of the PT grout specifications - Fluidity
Fluidity is measured using flow cones of different orifice diameters
  Flow cones of small orifices should be used
  Not suitable for thixotropic grouts with very low w/c ratio
  Grout spread gives a good indication of the fluidity and must be used
  Non-uniform pre-shear changes the fluidity
Retention of fluidity is measured for 30 minutes only
  Grouting operations can last for couple of hours after mixing
  Fluidity retention should be checked up to 3 hours

## Slide 40: Reasons for tendon corrosion and corrosion propagation are..
Chloride induced corrosion
  Chloride ions reach strands because of the incomplete fillings, voids, exposed strands
Carbonation induced corrosion
  Due to bad quality end caps and presence
  of voids
  Reduces the pH of the grout pore solution
Propagation due to the galvanic coupling
  Corroded region couples with passive region
Unwanted voids (formed due to bleed water) are the root cause for moisture/chloride ingress leading to strand corrosion in PT structures

## Slide 41: Effects of SCMs, superplasticizers and VMAs on the flow properties of grouts – a summary
Grout composition | Research findings | Reference
20 - 30 % fly ash SNF based SP | Plastic viscosity, yield stress, and bleed reduces | Khayat et al. 2008, Krishnamoorthy et al. 2002
5 - 20 % Silica fume SNF based SP & Cellulose based VMA | Fluidity decreases drastically Bleed can be reduced | Hope et al. 1988 Khayat et al. 1999 Sonebi et al. 2010
20 – 50 % GGBS & SMF based SP | Fluidity increases Bleed can be reduced | Bras et al. 2013
6 – 20 % Metakaolin PCE based SP & Polysaccharide VMA | Increased flow time, compressive strength and yield stress. Bleed reduces | Sonebi et al. 2013

## Slide 42: Test methods and the effect of temperature and humidity – a review
Grout composition | Research findings | Reference
OPC with special admixture | Admixture to control bleed Devised test methods Wick-induced bleed test Pressure induced bleed test | Schupack 1971,1974
5 - 20 % Silica fume, GGBS and SNF superplasticizer | Simple field test to assess the flow and washout loss | Khayat, 1998
10 – 20 % silica fume SNF superplasticizer | Grout fluidity increase with increase in temperature and humidity | Diedrichs, 1989

## Slide 43: Effect of inert fillers – a review
Grout composition | Research findings | Reference
Portland cement & PCE based superplasticizer | Indirect relationship of yield stress and bleed resistance, effect of chemical admixtures on the rheological parameters | Roussel, 2009 Nugyen, 2011
Portland cement, Limestone filler upto 45%, PCE based SP | Formation of soft grout | Hamilton et al. 2014
Soft grout layer at the top
Pre-packaged, highly flowable and bleed resistant grouts are not available in India and many parts of the world

## Slide 44: The following materials were identified for designing the grouts
Binders
  OPC 53 Grade
  Class F Fly ash – 621 m2/kg
  Class F Fly ash – 536 m2/kg
  Silica fume
Chemical additives
  PCE-based superplasticizer
  Cellulose-based VMA
  Nanoclay
1

## Slide 45: Physical properties of the binders
Property | OPC | Fly ash-1 | Fly ash-2 | Silica fume
Water demand for normal consistency of cement paste (%) | 30 | - | - | -
Initial setting time (minutes) | 175 | - | - | -
Final setting time (hours) | 275 | - | - | -
Specific surface area (m2/kg) | 310 | 628 | 536 | 15000
Specific gravity | 3.15 | 2.3 | 2.4 | 2.2
Mean diameter (µm) | 15 | 4.5 | 3.5 | 0.41

## Slide 46: Chemical composition of the binders
Chemical composition | Quantity (% by mass) |  |  | 
 | Cement | Fly ash 1 | Fly ash 2 | Silica fume
SiO2 | 20.88 | 59.32 | 60.56 | 96.8
Al2O3 | 5.54 | 29.95 | 32.67 | -
Fe2O3 | 4.71 | 4.32 | 4.44 | -
CaO | 61.70 | 1.28 | 1.41 | 0.4
MgO | 1.06 | 0.61 | 0.23 | -
(Na2O)e | 0.20 | 0.16 | 0.12 | -
LOI | 2.27 | - | - | -
Determined using XRF

## Slide 47: Physical properties of admixtures
Property | Superplasticizer | Viscosity modifying agent | Nanoclay
Commercial Name | Melflux 2651 F | Tylose MH | Acti-gel 208
Form | Powder | Powder | Powder
Colour | Yellow | White | Yellow
Odour | Odourless | Odourless | Odourless
Density (kg/m3) | 450 | 1300 | 1400
pH | 6.5 - 8.5 | 6 - 8 | 6-7
Drying loss | Maximum 2% | Maximum 1% | Maximum 1%

## Slide 48: Approximate binder compositions were obtained using particle packing approach (EMMA)
(OPC + FA1) mix
Particle packing method
Optimum gradation volume ratios
Modified Andreasson model (q = 0.23)

## Slide 49: The particle packing of the designs from EMMA were confirmed using Puntke test
20 cm3 of powder
Water is added gradually until the surface becomes glossy
  due to the layer of excess water
Packing density
VW = Vol. of water in cm3
VP = Vol. of powder (20 cm3)
Puntke test

## Slide 50: Puntke test results for the (OPC + FA1) mix
OPC (Vol %)
% Volume proportions | Packing density
50:50 | 0.600
55:45 | 0.614
58:42 | 0.618
60:40 | 0.611
65:35 | 0.608
70:30 | 0.604
(OPC + FA1) mix

## Slide 51: w/b, SP dosage, and VMA dosage were determined
Normal consistency test (Vicat apparatus) - w/b
Wick-induced bleed test - VMA dosage
Flow cone test – SP dosage
VMA (%) SP (%) | 0 | 0.02 | 0.03 | 0.04 | 0.05
0 | 58 | 62 | 78 | 81 | 97
0.07 | 37 | 51 | 65 | 71 | 82
0.08 | 25 | 37 | 57 | 62 | 71
0.09 | 20 | 28 | 48 | 59 | 64
0.10 | 18 | 23 | 31 | 41 | 48
0.11 | 10 | 12 | 17 | 22 | 25
0.12 | 10 | 12 | 16 | 21 | 23
VMA (%) SP (%) | 0 | 0.02 | 0.03 | 0.04 | 0.05
0 | 1.9 ml | 0 | 0 | 0 | 0
0.07 | 2.0 ml | 0 | 0 | 0 | 0
0.08 | 2.1 ml | 0 | 0 | 0 | 0
0.09 | 2.2 ml | 0 | 0 | 0 | 0
0.10 | 2.5 ml | 0 | 0 | 0 | 0
0.11 | 3.8 ml | 0 | 0 | 0 | 0
0.12 | 4.9 ml | 1 ml | 0.5 ml | 0 | 0
Effect of superplasticizer and VMA on bleed
Effect of Superplastizer and VMA on flow time

## Slide 52: SP dosage, and VMA dosage were determined - graphical representation
Effect of superplasticizer and VMA on bleed
Effect of Superplastizer and VMA on flow time

## Slide 53: Mixing procedure and sequence adopted
Dry blending of cement and mineral admixture in Hobart mixer
Add water to high shear mixer
Add the pre-blended grout material to the mixing water at 300 rpm
Increase speed to 1500 rpm and continue mixing
Sequence
Duration(s)
120
15
60
300
Control panel
3 HP motor
Mixing bowl
Kamalakannan et al. 2018; Bras et al. 2010

## Slide 54: Yield per bag and material cost were calculated
Grout | PPG1 | PPG2 | PPG3 | PPG4 | PPG5 | PPG6 | TF
Yield per 25 kg bag (l) | 15.28 | 15.48 | 15.84 | 15.60 | 16.11 | 15.74 | 15.84
No. of 25 kg bags for 1m3 grout | 63 | 63 | 64 | 63 | 64 | 63 | 64
Material cost per 25 kg bag (INR) | 193 | 208 | 200 | 237 | 225 | 217 | 200
Material cost for 1m3 of grout (INR) | 12631 | 13437 | 12706 | 14457 | 14175 | 13720 | 12706